###### Table 1 Review of explicit modelling of segmental tunnel lining

| Reference | Tunnel structure | Numerical model | Numerical software | Model validation against experimental / field data |
| --- | --- | --- | --- | --- |
| Gu (2011) | Concrete tunnel ring | 3D continuum bolt model and two tunnel rings | ABAQUS | No |
| Li et al., (2014) | Cast iron segmental joint | 3D continuum bolt model and development of bolt-spring model | ABAQUS | Yes |
| Li et al., (2015a, 2015b, 2016 ) | Cast iron tunnel | Simulation of large-scale tunnel structure using bolt-spring model | ABAQUS | Yes |
| Shi, et al. (2016) | Concrete tunnel subjected to adjacent deep excavation | 3D bolt model in discontinuous contact | ABAQUS | No |
| Jin et al.(2017) | Water-conveyance concrete tunnel segmental joint | 3D continuum bolt model | ABAQUS | Yes |
| Tsiampousi, et al., (2017) | Cast iron segmental joint | 3D continuum bolt model | Imperial College Finite Element Program (ICFEP) | Yes |
| Gong, et al. (2018, 2019) | Gasketed concrete tunnel segmental joint | 3D continuum gasket model | ABAQUS | Yes |

###### Table 2 Loading cases of the segmental joint bending tests

| Loading case | Axial compression N (kN/m) | Vertical load P3 (kN/m) | Equivalent bending moment M and eccentricity e0 |
| --- | --- | --- | --- |
| B1 | 2433 | 200 | M=-382 kNm/m, e0=-0.157 m (see Figure 2.a) |
| B2 | 4138 | 320 | M=-589 kNm/m, e0=-0.142 m (see Figure 2.a) |
| B3 | 1893 | 240 | M=447 kNm/m, e0=0.236 m (see Figure 2.b) |
| B4 | 3333 | 450 | M=796 kNm/m, e0=0.239 m (see Figure 2.b) |

###### Table 3 Concrete model characteristic values for Grade C55

| Grade | Density (g/cm3) |  | Modulus of elasticity E1 (MPa) | Modulus of hardening plasticity Er (MPa) |  | Poisson's ratio |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C55 | 2.5 | 35495 |  | 592 |  |  | 0.167 |  |
| Critical stress σb (MPa) | Strain (%) εb |  | Peak stress σc (MPa) |  | Strain (%) εc |  | Ultimate stress σd’ (MPa) | Strain (%) εd’ |
| 25.3 | 0.713 |  | 32.9 |  | 2 |  | 32.9 | 3.3 |

###### Table 4 Bolt material property (DIN EN ISO 898-1)

| Grade | Yield Strain | Rupture Strain | Yield Strength (MPa) | Tensile Strength (MPa) |
| --- | --- | --- | --- | --- |
| 5.8 | 0.0020 | 0.18 | 400 | 500 |
| 6.8 | 0.0024 | 0.18 | 480 | 600 |
| 8.8 | 0.0032 | 0.18 | 640 | 800 |

###### Table 5 Loading cases of the segmental joint shear tests

| Loading case | Axial compression F(kN/m) | Shear load P (kN) | Remark |
| --- | --- | --- | --- |
| S1 | 900 | 4500 kN | Shear in longitudinal direction (see Figure 6.a) |
| S2 | 450 | 2250 kN |  |
| S3 | 900 | 4500 kN | Shear in radial direction (see Figure 6.b) |
| S4 | 450 | 2250 kN |  |

Table 6 Comparison of computational time between bolt-spring models and continuum model

| Loading cases | Single spring model （hours） | Nine-spring model（hours） | Continuum model（hours） | Ratio a | Ratio b |
| --- | --- | --- | --- | --- | --- |
| 1 | 1.02 | 1.67 | 14.75 | 14.4 | 8.8 |
| 2 | 1.09 | 1.88 | 20.54 | 18.8 | 10.9 |
| 3 | 2.40 | 3.57 | 29.98 | 12.5 | 8.4 |
| 4 | 1.29 | 1.93 | 16.09 | 12.4 | 8.4 |
| 5 | 1.54 | 2.41 | 26.46 | 17.2 | 11.0 |
| 6 | 1.81 | 2.75 | 30.63 | 16.9 | 11.1 |

N.B. a is the ratio of the computational time for the continuum model to the single spring model, whilst b is the ratio of the computation time for the nine-spring model to the singe spring model.