Supplementary Information

- HRXRD Reciprocal Space Maps (RSM): symmetrical (004) reflection

Figure S1. HRXRD reciprocal space maps collected around the symmetrical (004) reflection for as deposited Ge1-xSnx/Ge/Si samples containing different Sn concentrations. Different reference lines are plotted to facilitate reading: horizontal green dashed lines indicate the reciprocal coordinate of vertically relaxed Ge layers, while the vertical black dashed line marks the [004] direction.

- Active carrier depth profile by SIMS and Van der Pauw-Hall measurements

Figure S2. Black curves are the SIMS Sb profiles reported in Figure 1 in the main manuscript at different laser energy density. Red curves are the ﻿active carrier depth profile obtained by the truncation of SIMS profiles to a certain maximum activation level in order to obtain an active carrier dose equal to the experimental values obtained by Van der Pauw-Hall electrical measurements. This procedure implies that the de-activation of Sb is located and related to an extremely high Sb concentration zone, as previously experimentally verified for Sb in Ge [1]. The maximum active concentration levels are reported in the manuscript in Table 1.

Table S1. Extension of Table 1 presented in the manuscript: sheet resistance (Rs), active carrier dose (Ns) and carrier mobility values are shown. These data were collected by Van der Pauw – Hall measuments.

| Sample | Laser energy density (mJ/cm2) | Rs (Ω/sq.) | Ns (1015 cm-2) | Mobility (cm2/Vs) |
| --- | --- | --- | --- | --- |
| Ge0.916Sn0.084 | - | - | - | - |
| Ge0.906Sn0.094 | - | - | - | - |
| Ge0.906Sn0.094 | 500 | - | - | - |
| Ge0.916Sn0.084:Sb | 400 | 29.2 ± 1.5 | 4.21 ± 0.4 | 50.5 ± 6.1 |
| Ge0.916Sn0.084:Sb | 500 | 26.3 ± 1.3 | 4.82 ± 0.5 | 49.2 ± 5.9 |
| Ge0.916Sn0.084:Sb | 600 | 30.0 ± 1.5 | 4.40 ± 0.4 | 47.3 ± 5.7 |
| Ge0.906Sn0.094:Sb | 700 | 15.3 ± 1.4 | 7.41 ± 0.4 | 55.1 ± 5.3 |

Bibliography

[1] Carraro, C., Milazzo, R., Sgarbossa, F., Fontana, D., Maggioni, G., Raniero, W., … Napolitani, E. «N-type heavy doping with ultralow resistivity in Ge by Sb deposition and pulsed laser melting» Applied Surface Science, 509 (2020) 145229.