Supplementary Information

Low-Temperature Ionic Layer Adsorption and Reaction Grown Anatase TiO2 Nanocrystalline Films for Efficient Perovskite Solar Cell and Gas Sensor Applications

Shoyebmohamad F. Shaikh,1 Balaji G. Ghule1 Umesh T. Nakate 1 Pritamkumar V. Shinde,1 Satish U. Ekar,1 Colm O’Dwyer 2* Kwang Ho Kim3*nd Rajaram S. Mane1*

1School of Physical Sciences, Swami Ramanand Teerth Marathwada University, Nanded, 431 606, India

2School of Chemistry, University College of Cork, Cork T12 YN 60, Ireland.

2Micro-Nano Systems Centre, Tyndall National Institute, Lee Maltings, Cork T12 R5CP, Ireland.

2Environmental Research Institute, University College Cork, Lee Road, Cork T23 XE10, Ireland.

3National Core Research for Hybrid Materials Solution, Pusan National University, Busan 600-735, Republic of Korea.

Fig. S1 Binding energy survey spectra of TiO2 nanostructure film.

Fig. S2 BET adsorption-desorption isotherm for TiO2 nanostructure powder.

Fig. S3 UV-vis absorbance spectra of TiO2 ETL before the deposition of perovskite. The inset Tauc plot shows the band gap position of the TiO2 ETL.

Fig. S4 JV characteristics of the FTO/TiO2 ETL/perovskite/spiro-OMeTAD /gold device under illumination of simulated AM1.5G light (100 mW cm-2). The TiO2 ETL varied using different SILAR Cycle layers times of 10, 15 and 20 Cycle. The scan rate was constant at 8.6 mV s-1 for all the measurements.

Fig. S5 Device parameter statistics demonstrating the consistency in the performance of 10 devices: (a) JSC, (b) VOC, (c) ff, and (d) PCE of FTO/TiO2/perovskite/spiro-OMeTAD/gold. The 25th, 50th, and 75th percentiles of the device parameters are represented with three horizontal lines in the box. The average and maximum/minimum values are denoted by ■ and ×, respectively.

Fig. S6 JV characteristics of forward scan and reverse scan for FTO/TiO2 ETL/perovskite /spiro-OMeTAD/ gold device under illumination of simulated AM1.5G light (100 mW cm-2) for scan rates of (a) 520, (b) 52, and (c) 8.7 mV s-1.

Table S1 Structural parameters of TiO2 nanostructures film.

| Molar concentration | Standard values/Formula | (hkl) | Estimated Values (nm) |
| --- | --- | --- | --- |
| Crystallite size (D) (nm) Scherrer’s formula |  | 101 004 200 105 | 8 6 7 8 |
| Average crystallite size |  |  | 7.2 |
| d – spacing (Å) JCPDS - Card no. 21-1272 | 3.5168 2.3782 1.8925 1.6999 | 101 004 200 105 | 3.5408 2.3948 1.8994 1.6789 |
| Diffraction peak 2θ (0) | 25.281 37.800 48.049 53.890 | 101 004 200 105 | 25.119 37.510 47.830 53.990 |
| Dislocation density (lines/m2) X 1015 | δ = 1/D2 | 101 004 200 105 | 15.625 27.777 15.625 40.000 |
| Texture coefficient TC | TChkl=IhklI01NIhklI0 | 101 004 200 105 | 2.011 1.373 0.492 1.124 |
| Micro strain () | cosθλ = 1D+sinθλ |  | 12.6 x 10-3 |

Table S2 The BET surface area and pore size distribution analysis.

| Surface Area | Pore Volume | Average Pore Diameter |
| --- | --- | --- |
| 120.53 m2g-1 | 0.197 cm3g-1 | 6.53 nm |

Table S3 Summary of photovoltaic performances of the FTO/TiO2 ETL/perovskite/spiro-OMeTAD/gold devices fabricated by various SILAR cycle under AM 1.5 illumination (100 mW cm-2).

| ETL | JSC (mA cm-2) | VOC (V) | ff (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| TiO2- 10 cycle | 19.5 | 0.80 | 59.6 | 8.5 |
| TiO2- 15 cycle | 18.0 | 0.81 | 66.3 | 9.7 |
| TiO2- 20 cycle | 19.1 | 0.68 | 53.3 | 7.0 |

Table S4 Comparative study of TiO2 with different synthesis method for perovskite solar cell application.

| ETL | Phase | Morphology | Synthesis Method | PCE | References |
| --- | --- | --- | --- | --- | --- |
| TiO2 | Rutile | Rod | Hydrothermal | 8.1 | 30 |
|  | Anatase | Spherical |  | 7.2 |  |
|  | Rutile | Nanorod | Hydrothermal | 9.4 | 31 |
|  | Rutile | Nanorod | Hydrothermal | 7.9 | 32 |
|  | NA | Irregular | Electrodeposition | 13.6 | 33 |
|  | Rutile | Nanograin | Chemical Bath Deposition | 11.1 | 34 |
|  | NA | Nanocrystal | Sol-gel | 11.4 | 35 |
|  | Anatase | Spherical | SILAR | 9.7 | This work |

Table S5: The comparison of reported sensor performances of different materials used for ammonia gas detection.

| Sensor Material | Synthesis Method | C (ppm) | S (%) | T (°C) | Reference |
| --- | --- | --- | --- | --- | --- |
| Functionalised SWCNT | Magnetron sputtering | 50 | 20.2 | 27 | 33 |
| MWCNT–PEDOT:PSS | Solution casting | 50 | 16 | 27 | 34 |
| CNT | Chemical vapour deposition | 100 | 1.5 | 27 | 35 |
| Graphene/polyaniline | Polymerisation | 100 | 10 | 27 | 36 |
| BAX-CS1% | Polymer-derived | 500 | 21 | 27 | 37 |
| Anatase-TiO2 | SILAR | 100 | 80 | 27 | This work |

Table S6: Comparison of gas sensor responses based on TiO2 for different gas detection. (C-Concentration (ppm), S-Response (%), T-Temperature (°C)).

| Sensor Material | Synthesis Method | Target gas | C (ppm) | S (%) | T (°C) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| TiO2 Nanotubes | Anodization | H-CHO | 50 | 40 | 27 | 38 |
| TiO2 Nanotubes | Anodization | O2 | 200 | 100 | 50 | 39 |
| p-PANI/n-TiO2 | CBD/ED | LPG | 0.1 (Vol. %) | 60 | 27 | 40 |
| TiO2 | Anodization | H2 | 1000 | 170 | 150 | 41 |
| TiO2 Nanotubes | Anodization | CHCl3 | 1000 | 98.5 | 27 | 42 |
| Anatase-TiO2 | SILAR | NH3 | 100 | 80 | 27 | This work |

Table S7 Photovoltaic parameters of FTO/TiO2 ETL/perovskite/spiro-OMeTAD/Au device as a function of scan rate and scan direction.

| Scan rate (mV s-1) | Scan direction | Jsc (mA cm-2) | Voc (V) | ff (%) | η (%) |
| --- | --- | --- | --- | --- | --- |
| 520 | Reverse | 18.7 | 0.83 | 58.2 | 8.5 |
|  | Forward | 18.3 | 0.81 | 48.3 | 6.8 |
| 52 | Reverse | 18.1 | 0.82 | 61.2 | 9.0 |
|  | Forward | 17.8 | 0.81 | 58.5 | 7.5 |
| 8.7 | Reverse | 18.2 | 0.81 | 66.3 | 9.7 |
|  | Forward | 18.1 | 0.81 | 60.1 | 9.1 |