SUPPLEMENTARY INFORMATION

Honeycomb micro/nano-architecture of stable β-NiMoO4 electrode/catalyst for sustainable energy storage and conversion devices

N. Padmanathana,b, Han Shaoa and Kafil M. Razeeba*

aMicro-Nano Systems Centre, Tyndall National Institute, University College Cork, Dyke Parade, Lee Maltings, Cork T12 R5CP, Ireland

bDepartment of Physics, Karpagam Academy of Higher Education, Coimbatore – 641021, Tamilnadu, India.

*Corresponding Author: kafil.mahmood@tyndall.ie

Fig. S1 XRD pattern of pure NF and hydrothermally grown β-NiMoO4-NF.

Fig. S2 EDS spectrum of β-NiMoO4-NF.

Fig. S3 (a) Linear plot of square root of scan rate and specific current at peak potential (b) Linear relationship graph of log Ipa and log v (c) Power law fitting plot between square root of scan rate and Peak current/square root of v and (d) Ratio of faradaic contribution and capacitive contribution in β-NiMoO4-NF electrode.

Fig. S4 Charge/discharge profile at high specific current 15 – 50 mAcm-2 and (b) Variation of specific capacity with respect to different specific current.

Table S1: Comparison of specific capacitance values for different electrodes.

| Electrode | Specific Capacitance (Fg-1) | Current Density | Capacity Retention | References |
| --- | --- | --- | --- | --- |
| NiMoO4/MWCNTs | 805 | 1 Ag-1 | 66.7% after 2000 cycles | [1] |
| NiMoO4/CoMoO4 | 740 | 1 Ag-1 | 89.1% after 2000 cycles | [2] |
| NiMoO4 | 3412 | 1 Ag-1 | 31% after 2000 cycles | [3] |
| NiMoO4@CC | 970 | 2.5 Ag-1 | 91.3% after 5000 cycles | [4] |
| Ni@NiO/N-C | 1045 | 1 Ag-1 | 60% after 10000 cycles | [5] |
| NiMoO4 | 594 | 1 Ag-1 | 56% after 1000 cycles | [6] |
| C@NiMoO4 | 268.8 | 1 Ag-1 | 88.4% after 2000 cycles | [7] |
| NiMoO4 | 999 | 1 Ag-1 | - | [8] |
| NiMoO4 | 1102 | 1 Ag-1 | 90% after 1000 cycles | [9] |
| β- NiMoO4@NF | 916 | 5 mAcm-2 | 89.7% after 5000 cycles | This work |

EIS studies of Symmetric Cell

Fig. S5 (a) Nyquist plot of β-NiMoO4-NF||β-NiMoO4-NF supercapattery and (b) the corresponding extended view of high frequency region.

Fig. S5(a) shows the EIS spectra of the symmetric cell, which has a small semicircle (see magnified view in Fig. S5(b)), followed by inclined line at the high and low frequency regions, respectively. The inset shows the corresponding equivalent circuit used to relate the observed Nyquist plot. From the EIS data, it can be seen that the solution resistance (Rs) accompanying with charge transfer resistance (Rct) and the Warburg impedance (W).  The magnified view of high frequency region is shown in Fig. S5(b) clearly evidences the small semicircle like region, which denotes a very low charge transfer resistance (1.22 Ω) even after 5,000 cycles, confirming good electrical conductivity of the electrodes [10]. In the low frequency region, the sloped line infers the proton diffusion into the bulk electrode. Additionally, the low frequency tail makes an angle of nearly 45º at real axis further evidences the fast diffusion of electrolyte ion and battery like behaviour of the device [11].

EIS analysis of MOR studies

Fig. S6 (a) Electrochemical impedance spectra MOR for β-NiMoO4-NF catalyst and corresponding equivalent circuit (inset) (b) The extended view of high frequency region.

The excellent methanol oxidation behavior of this β-NiMoO4-NF nanostructure was evaluated with the electrochemical impedance spectra (EIS). Figure S6 (a & b) (SI) shows the EIS spectra of the β-NiMoO4-NF electrode with and without the supporting methanol electrolyte additive. The observed Nyquist plot consists of small semi-circular like portion at high frequency region (Fig. S6 (b)) and extended tail at low frequency region related to the charge transfer resistance and capacitance over the metal oxide surface, respectively. The corresponding equivalent circuit to fit the impedance spectra gives the appropriate solution resistance (Rs), capacitance (Cdl), charge transfer resistance (Rct) and Warburg impedance (W) [12]. From the EIS spectra, it can be observed that the Rct value has been increased slightly during methanol oxidation process due to methanol adsorption. After adding 1 M CH3OH, the estimated solution resistance after the first and 1000 cycles are found to be same ~2.49 Ω and the corresponding Rct value do not change, which is ~3.52 Ω. This indicates that our β-NiMoO4-NF can tolerant methanol adsorption or oxidation of intermediates and maintain an excellent conductivity. The resulting low Rct value stems from the ambipolar conductivity of the β-NiMoO4-NF honeycomb architecture with good mechanical integrity between NF and metal oxide.

Table S2: Comparison of OER and HER overpotential @ 10 mAcm-2 for different catalysts.

| Catalyst | OER overpotential @ 10 mAcm-2 | Reference | Catalyst | HER overpotential @ 10 mAcm-2 | Reference |
| --- | --- | --- | --- | --- | --- |
| NiCoP/CNF | 268 mV | [13] | Co-Cl4 -MOF | 283 mV | [22] |
| NiCo2O4 @NiMoO4 | 340 mV | [14] | CoMoO4 | 353 mV | [23] |
| NiMoO4 | 340 mV | [15] | CoS2@Co3O4 | 320 mV | [24] |
| NiO@NiMoO4 | 280 mV | [16] | Cu2MoS4 | 360 mV | [25] |
| Ni@NiO/N-C | 390 mV | [17] | MoS2 | 450 mV | [26] |
| NiMoO4 | 370 mV | [18] | Ni, Co, NiCo | 333, 430 mV | [27] |
| β-Ni(OH)2 | 340 mV | [19] | NiS2 | 302 mV | [28] |
| Ni3S2 | 312 mV | [20] | Ni3Se2/NiSe | 260 mV | [29] |
| NiCo2S4 | 400 mV | [21] | Ni CNF | 921 mV | [30] |
| β- NiMoO4 | 351 mV | This work | β- NiMoO4 | 238 mV | This work |

References

[1] Zhang Y, Chang C-r, Jia X-d, Huo Q-y, Gao H-l, Yan J, et al. Morphology-dependent NiMoO4/carbon composites for high performance supercapacitors. Inorganic Chemistry Communications. 2020;111:107631.

[2] Zhang Y, Chang C-r, Jia X-d, Cao Y, Yan J, Luo H-w, et al. Influence of metallic oxide on the morphology and enhanced supercapacitive performance of NiMoO4 electrode material. Inorganic Chemistry Communications. 2020;112:107697.

[3] Yong Zhang, Hai-li Gao, Xiao-dong Jia, Shi-wen Wang, Ji Yan, He-wei Luo, Ke-zheng Gao, Hua Fang, Ai-qin Zhang, and Li-zhen Wang, NiMoO4 nanorods supported on nickel foam for high-performance supercapacitor electrode materials. Journal of Renewable and Sustainable Energy.2018; 10:054101.

[4] Hussain S, Javed MS, Asim S, Shaheen A, Khan AJ, Abbas Y, Ullah N, Iqbal A, Wang M, Qiao G, Yun S. Novel gravel-like NiMoO4 nanoparticles on carbon cloth for outstanding supercapacitor applications. Ceramics International. 2020; 46(5):6406-12.

[5] Hao Y, Huang H, Wang Q, Wang Q, Zhou G. Nitrogen-doped carbon/NiMoO4 nanospheres assembled by nanosheets and ultrasmall nanoparticles for supercapacitors. Chemical Physics Letters. 2019;728:215-23.

[6] Neeraj NS, Mordina B, Srivastava AK, Mukhopadhyay K, Prasad NE. Impact of process conditions on the electrochemical performances of NiMoO4 nanorods and activated carbon based asymmetric supercapacitor. Applied Surface Science. 2019;473:807-19.

[7] Wei C, Huang Y, Yan J, Chen X, Zhang X. Synthesis of hierarchical carbon sphere@ NiMoO4 composite materials for supercapacitor electrodes. Ceramics International. 2016 ;42(14):15694-700.

[8] Jinlong L, Miura H, Meng Y. A novel mesoporous NiMoO4@ rGO nanostructure for supercapacitor applications. Materials Letters. 2017;194:94-7.

[9] Lin L, Liu T, Liu J, Sun R, Hao J, Ji K, Wang Z. Facile synthesis of groove-like NiMoO4 hollow nanorods for high-performance supercapacitors. Applied Surface Science. 2016;360:234-9.

[10] Padmanathan N, Shao H, McNulty D, O'Dwyer C, Razeeb KM. Hierarchical NiO–In2O3 microflower (3D)/nanorod (1D) hetero-architecture as a supercapattery electrode with excellent cyclic stability. Journal of Materials Chemistry A. 2016;4(13):4820-30.

[11] Sankar KV, Seo Y, Lee SC, Liu S, Kundu A, Ray C, Jun SC. Cobalt carbonate hydroxides as advanced battery-type materials for supercapatteries: Influence of morphology on performance. Electrochimica Acta. 2018;259:1037-44.

[12] Gu CD, Huang ML, Ge X, Zheng H, Wang XL, Tu JP. NiO electrode for methanol electro-oxidation: Mesoporous vs. nanoparticulate. international journal of hydrogen energy. 2014;39(21):10892-901.

[13] Surendran S, Shanmugapriya S, Sivanantham A, Shanmugam S, Kalai Selvan R. Electrospun carbon nanofibers encapsulated with NiCoP: a multifunctional electrode for supercapattery and oxygen reduction, oxygen evolution, and hydrogen evolution reactions. Advanced Energy Materials. 2018;8(20):1800555.

[14] Du X, Fu J, Zhang X. NiCo2O4@NiMoO4 supported on nickel foam for electrocatalytic water splitting. ChemCatChem. 2018;10(23):5533-40.

[15] Zhao X, Meng J, Yan Z, Cheng F, Chen J. Nanostructured NiMoO4 as active electrocatalyst for oxygen evolution. Chinese Chemical Letters. 2019;30(2):319-23.

[16] Jia D, Gao H, Xing L, Chen X, Dong W, Huang X, Wang G. 3D Self-Supported Porous NiO@ NiMoO4 Core–Shell Nanosheets for Highly Efficient Oxygen Evolution Reaction. Inorganic chemistry. 2019;58(10):6758-64.

[17]  Xie A, Zhang J, Tao X, Zhang J, Wei B, Peng W, Tao Y, Luo S. Nickel-based MOF derived Ni@ NiO/N–C nanowires with core-shell structure for oxygen evolution reaction. Electrochimica Acta. 2019;324:134814.

[18] Zhang S, She G, Li S, Qu F, Mu L, Shi W. Enhancing the electrocatalytic activity of NiMoO4 through a post-phosphorization process for oxygen evolution reaction. Catalysis Communications. 2019;129:105725.

[19] Kim N, Lim D, Choi Y, Shim SE, Baeck SH. Hexagonal β-Ni(OH)2 nanoplates with oxygen vacancies as efficient catalysts for the oxygen evolution reaction. Electrochimica Acta. 2019;324:134868.

[20] Ren G, Hao Q, Mao J, Liang L, Liu H, Liu C, Zhang J. Ultrafast fabrication of nickel sulfide film on Ni foam for efficient overall water splitting. Nanoscale. 2018;10(36):17347-53.

[21] Feng X, Jiao Q, Cui H, Yin M, Li Q, Zhao Y, Li H, Zhou W, Feng C. One-pot synthesis of NiCo2S4 hollow spheres via sequential ion-exchange as an enhanced oxygen bifunctional electrocatalyst in alkaline solution. ACS applied materials & interfaces. 2018;10(35):29521-31.

[22] Li YS, Yi JW, Wei JH, Wu YP, Li B, Liu S, Jiang C, Yu HG, Li DS. Three 2D polyhalogenated Co (II)-based MOFs: Syntheses, crystal structure and electrocatalytic hydrogen evolution reaction. Journal of Solid State Chemistry. 2020;281:121052.

[23] Yan X, Tian L, Atkins S, Liu Y, Murowchick J, Chen X. Converting CoMoO4 into CoO/MoO x for overall water splitting by hydrogenation. ACS Sustainable Chemistry & Engineering. 2016;4(7):3743-9.

[24] Aftab U, Tahira A, Samo AH, Abro MI, Baloch MM, Kumar M, Ibupoto ZH. Mixed CoS2@Co3O4 composite material: An efficient nonprecious electrocatalyst for hydrogen evolution reaction. International Journal of Hydrogen Energy. 2020;45: 13805-13813

[25] Xue M, Wei Y, Liu G. Facile hydrothermal preparation of edge-oriented Cu2MoS4 as an efficient electrocatalyst for hydrogen evolution reaction. Materials Letters. 2019;256:126663.

[26] Lai B, Singh SC, Bindra JK, Saraj CS, Shukla A, Yadav TP, Wu W, McGill SA, Dalal NS, Srivastava A, Guo C. Hydrogen evolution reaction from bare and surface-functionalized few-layered MoS2 nanosheets in acidic and alkaline electrolytes. Materials Today Chemistry. 2019;14:100207.

[27] Dahonog LA, Balela MD. Electroless Deposition of Nickel-Cobalt Nanoparticles for Hydrogen Evolution Reaction. Materials Today: Proceedings. 2020;22:268-74.

[28] Liang Y, Yang Y, Xu K, Yu T, Yao S, Peng Q, Yuan C. Crystal plane dependent electrocatalytic performance of NiS2 nanocrystals for hydrogen evolution reaction. Journal of Catalysis. 2020;381:63-9.

[29] Wang HB, Sun YS, Ma F, Zhou L, Li HF, Zhang L, Chen GJ, Xu YK, Chen YN, Xu KW, Ma DY. Se molarity tuned composition and configuration of Ni3Se2/NiSe core-shell nanowire heterostructures for hydrogen evolution reaction. Journal of Alloys and Compounds. 2020;819:153056.

[30] Chen J, Wang J, Chen J, Wang L. A bifunctional electrocatalyst of PtNi nanoparticles immobilized on three-dimensional carbon nanofiber mats for efficient and stable water splitting in both acid and basic media. Journal of Materials Science. 2017;52(22):13064-77.