# Impact of Copper Doping on the Anatase to Rutile Transition of TiO2 Photocatalysts

Ciara Byrne a,b, Lorraine Moran c, Daphne Hermosilla d, Noemí Merayo e, Ángeles Blanco e, Stephen Rhatiganf, Michael Nolan f, Steven Hinder g, Priyanka Ganguly a,b and Suresh C. Pillai a,b†

a Nanotechnology and Bio-engineering Research Group, Department of Environmental Science, Institute of Technology Sligo, Sligo, Ireland

b Centre for Precision Engineering, Materials and Manufacturing Research (PEM), Institute of Technology Sligo, Sligo, Ireland.

c Department of Life Sciences, Institute of Technology Sligo, Sligo, Ireland

d University of Valladolid, E.U. Ingenierías Agrarias de Soria, Campus Duques de Soria, 42005 Soria, Spain.

e Complutense University of Madrid, FCC Químicas, Ciudad Universitaria s/n, 28040 Madrid, Spain.

f Tyndall National Institute, University College Cork, Lee Maltings, Dyke Parade, Cork, Ireland

g The Surface Analysis Laboratory, Faculty of Engineering and Physical Sciences, University of Surrey, Guildford, Surrey, GU2 7XH, United Kingdom

† Corresponding author. E-mail address: pillai.suresh@itsligo.ie

## Supplementary Information

Figure S1: XRD of all uncalcined samples. (a) 0% copper (b) 2% copper (c) 4% copper and (d) 8% copper, where A= anatase and R = Rutile.

Figure S2: XRD of all samples calcined at 600°C. (a) 0% copper (b) 2% copper (c) 4% copper and (d) 8% copper, where A= anatase and R = Rutile.

Figure S3: XRD of all samples calcined at 700°C. (a) 0% copper (b) 2% copper (c) 4% copper and (d) 8% copper, where A= anatase and R = Rutile.

Figure S4: Raman spectra of 8% Cu-TiO2 calcined at 600 °C, 650 °C and 700 °C.

Table S1: The elemental composition (in atomic %) of the elements present which have been derived from XPS data.

|  | 0% Cu | 2% Cu | 4% Cu | 8% Cu |
| --- | --- | --- | --- | --- |
| C1s | 600 °C – 17.90% 650 °C – 24.81% 700 °C –26.76% | 600 °C – 13.64% 650 °C – 22.15% 700 °C –10.48% | 600 °C – 12.37% 650 °C – 25.80% 700 °C – 12.89% | 600 °C – 14.92% 650 °C – 24.89% 700 °C – 26.83% |
| O1s | 600 °C – 58.42% 650 °C – 53.90% 700 °C – 52.59% | 600 °C – 61.82% 650 °C – 53.53% 700 °C – 61.20% | 600 °C – 62.47% 650 °C – 51.12% 700 °C – 59.78% | 600 °C – 58.26% 650 °C – 51.98% 700 °C – 49.80% |
| Ti2p | 600 °C – 23.67% 650 °C – 21.29% 700 °C – 20.56% | 600 °C – 21.03% 650 °C – 19.49% 700 °C – 21.02% | 600 °C – 21.72% 650 °C – 18.51% 700 °C – 20.27% | 600 °C – 15.45% 650 °C – 18.05% 700 °C – 17.58% |
| S2p | N/A | 600 °C – 1.58% 650 °C – 1.02% 700 °C – 0.90% | 600 °C – 1.45% 650 °C – 0.79% 700 °C – 1.07% | 600 °C – 4.42% 650 °C – 1.51% 700 °C – 0.94% |
| Cu2p3 | N/A | 600 °C – 1.94% 650 °C – 3.82% 700 °C – 6.40% | 600 °C – 1.99% 650 °C – 3.60% 700 °C – 5.98% | 600 °C – 6.94% 650 °C – 3.58% 700 °C – 4.85% |

Table S2: XPS binding energy (eV) data for samples calcined at 600, 650 and 700°C

|  | 0% Cu | 2% Cu | 4% Cu | 8% Cu |
| --- | --- | --- | --- | --- |
| C1s | 600 °C – 284.9 650 °C – 284.9 700 °C – 284.9 | 600 °C – 284.9 650 °C – 284.9 700 °C – 284.9 | 600 °C – 285.0 650 °C – 284.9 700 °C – 285.0 | 600 °C – 285.0 650 °C – 284.9 700 °C – 284.9 |
| O1s | 600 °C – 530.2 650 °C – 530.0 700 °C – 530.1 | 600 °C – 530.5 650 °C – 530.2 700 °C – 529.2 | 600 °C – 530.4 650 °C – 530.1 700 °C – 530.3 | 600 °C – 530.5 650 °C – 530.3 700 °C – 530.1 |
| Ti2p | 600 °C – 459.0 650 °C – 458.8 700 °C – 458.9 | 600 °C – 459.2 650 °C – 458.9 700 °C – 458.9 | 600 °C – 459.1 650 °C – 458.9 700 °C – 458.9 | 600 °C – 459.0 650 °C – 459.0 700 °C – 458.8 |
| S2p | N/A | 600 °C – 169.5 650 °C – 168.9 700 °C – 168.9 | 600 °C – 169.2 650 °C – 168.9 700 °C – 169.3 | 600 °C – 169.6 650 °C – 169.1 700 °C – 168.9 |
| Cu2p3 | N/A | 600 °C – 933.0 650 °C – 932.8 700 °C – 933.2 | 600 °C – 932.9 650 °C – 932.8 700 °C – 933.3 | 600 °C – 934.0 650 °C – 932.9 700 °C – 933.9 |

Table S3: Deconvoluted XPS data (binding energy (eV)) for O1s, S2p and Cu2p3 for the 8% Cu-TiO2 samples

|  | 600 °C | 650 °C | 700 °C |
| --- | --- | --- | --- |
| O1s | 530.4 532.6 | 530.2 532.0 | 530.1 531.7 |
| S2p | 169.2 170.4 | 168.8 170.1 | 168.7 170.0 |
| Cu2p3 | 933.1 936.1 941.8 944.9 | 932.6 935.1 941.1 943.5 | 932.6 934.6 941.8 944.1 |

Figure S5: SEM image and EDX composition results of 0% Cu-TiO2 @ 500°C.

Figure S6: SEM image and EDX composition results of 8% Cu-TiO2 @ 500°C.

Figure S7: Local atomic structure in the vicinity of the dopant for (a) rutile and (b) anatase. Copper is represented by a blue sphere, titanium is grey and oxygen is red. The yellow sphere marks the location of the oxygen hole polaron.

Figure S8: Effect of T of the catalyst on both 1,4-dioxane and TOC removals.

Figure S9: Effect of Cu percentage in the removal efficiency of 1,4 dioxane.