Fabrication of a sensitive amperometric sensor for NADH and H2O2 using palladium nanoparticles-multiwalled carbon nanotubes nanohybrid

Hassan Hamidi a* and Behzad Haghighi b,c

a 	Department of Chemistry, Islamic Azad University of Zanjan, P.O. Box 49195-467, Zanjan, Iran.

b 	Department of Chemistry, Institute for Advanced Studies in Basic Sciences, P.O. Box 45195-1159, Gava Zang, Zanjan, Iran.

c	Department of Chemistry, College of Sciences, Shiraz University, Shiraz 71454, Iran.

A

Fig. S1

B

SEM images of GCE (A) and GCE/PdNPs-MWCNTs (B).

Fig. S2 Cyclic voltammograms for a PdNPs-MWCNTs/GCE in 0.5 M H2SO4 solution at a scan rate of 50 mV s-1

Fig. S3 The plot of peak current versus PdNPs-MWCNTs amount (mg mL-1 in DMF) obtained from cyclic voltammetric studies in 0.1 M KCl solution containing 1 mM K3Fe(CN)6 at a scan rate of 50 mV s-1.

Fig. S4 The plot of current response versus pH obtained from amperometric studies in the presence of 10 µM NADH. Conditions: supporting electrolyte, Ar-saturated phosphate buffer solution (0.1 M, pH 7.4); operating potential: +0.45 mV versus Ag|AgCl|KClsat; rotating speed: 2000 rpm

Fig. S5 The plot of current response versus pH obtained from amperometric studies in the presence of 10 µM H2O2. Conditions: supporting electrolyte, Ar-saturated phosphate buffer solution (0.1 M, pH 7.4); operating potential: +0.35 mV versus Ag|AgCl|KClsat; rotating speed: 2000 rpm.

Fig. S6 Lineweaver-Burk plot for glucose at Nafion/GOx/PdNPs-MWCNTs/GCE (in pH 7.4 phosphate buffer and at the applied potential of +0.350 V vs. Ag|AgCl|KClsat).

Corresponding authors:

Tel: +98 24 3346 1001, Fax: +98 24 3346 0037 (H. Hamidi)

E-mail address: hamidi.h@hotmail.com (H. Hamidi)

Tel: +98 71 3613 7178, Fax: +98 71 3646 0724 (B. Haghighi)

E-mail address: bhaghighi@shirazu.ac.ir (B. Haghighi))